[image: image1.png]HUIGUANG



PRODUCT INFORMATION

MEILOSE
GMC－5213
Product description 

GMC－5213 is a modified hydroxypropyl methyl cellulose (HPMC)  

Application / Advantages 

GMC－5213 was developed for gypsum-based applications, like gypsum hand plaster and gypsum finishing plaster. It imparts well-balanced properties, e.g. 
• high water demand
• good sag resistance
• improve the rheology of the plaster
• good consistency

• thermal stability improved
• good workability(no lump) : easy use
• good water retention 

It also imparts good workability and enhances water retention. The selected particle size distribution guarantees quick or lump free dissolution. It is compatible with all conventional mineral and organic binders. 

Specifications

	Form
	Powder
	

	Solubility
	Water soluble
	

	Viscosity1
	20,000~30,000 MPa·s
	Brookfield RV

	pH
	6.0~8.0 (2% solution)
	

	Moisture content
	Max. 8%
	ASTM D1347-72

	Particle size
	<125μm: min. 95%
	


Note: 1)The viscosities and other values shown are typical values for your guidance. They are not to be taken

as specification and are subject to certain variability. Please consult the sales specification for details.

    2)2% solution in water, Haake Rotovisko RV 100, shear rate 2.55/s, 20℃
Health
MEILOSE products have had extensive evaluation in both acute and long-term studies in a number of species, including humans. Their many years of use attest to their safety in a wide variety of applications. While the dust may cause mechanical irritation to the skin and eyes under extreme conditions, the products are considered to present no significant health hazard under normal handling conditions. 

Flammability 


Cellulose ether products are organic polymers that will burn when exposed to heat and a sufficient oxygen supply. Fires can be extinguished by conventional means avoiding any raising of dust by strong water jets. Huiguang recommends the use of water spray, carbon dioxide, or powder extinguishers. MEILOSE starts to decompose at about 200°C. Its ignition temperature is >360°C. MEILOSE burns easily and the fire may spread. Additionally, MEILOSE products, like other organic chemicals, should not be stored next to peroxides or other oxidizing agents. 

Packaging and Storage
MEILOSE GMC-5213 is packed in multiply paper bags with an inner polyethylene bag. Net weight 20KG (approx 44 lbs) or 25KG (approx 55 lbs). We recommend emptying the bags from the bottom. He empty bags can be recycled or burned. Unopened bags, MEILOSE GMC-5213 can be stored for several years. In opened bags, the moisture content of MEILOSE GMC-5213 will be influenced by the air humidity.
When stored in closed containers, or in its original packaging in a dry place at room temperature,

MEILOSE can be kept for a long time. In the case of high viscosity grades, a slow loss of viscosity can be measured after lengthy storage (>1 year). MEILOSE absorbs water from moist air. Once opened, container must be resealed and kept tightly closed. 








Shanghai Huiguang Fine Chemical Industry Co., Ltd
Address:No.888Muhua North Rode Fengxian Subarea Shanghai Chemical
Industry Part Shanghai. China Tel: +86-21-57448208  Fax: +86-21-57448209

www.shhuiguang.com 

