[image: image1]                 
                      江 苏 极 易 新 材 料  有  限  公  司

          Jiangsu Jiyi New Material Co.,Ltd
[image: image2.png]




JYANOX-1024
· Chemical Name: Benzene propanoic acid, 3 , 5-bis(1,1-dimethylethyl)-4-hydroxy-2- {3-[3,5-bis(1,1 -dimethylethyl )-4-hydroxyphenyl ]-1-oxopropyl }hydrazide

· Molecular Weight:  M=552.80
· Molecular Formula: C34H52N2O4
· [image: image3.png]OH

HO



Chemical Structure Formula:
· Typical Physical Properties:
	Item
	Standard 

	Appearance 
	   White Powder 

	Melting Range (℃)
	   224～229

	Volatile (%)
	   ≤  0.5

	Light Transmittance
	425nm, %
	   ≥  97

	
	500nm, %
	   ≥  99

	Ash Content
	     ≤  0.1

	Purity (%)
	   ≥  98


· Applications: It can be widely used for PE, PP, PA and so on, especially used mainly in wire and cable 
insulation .It is a characteristic of nondiscoloring and has a good synergistic effect with general antioxidant. The dosage is recommended to be 0.1%~0.5%.
· Storage: Stable in property. No special repuirement but keep away from damp or heat.
· Packing: It is packed in cardboard box lined with plastic bags with the net capacity of 20 kg. It can also be designed according to customers' requirements.

[image: image1]
  Address: North of North Ring Road and West of Dongcheng Road, Economic Development Zone of Fengxian, Xuzhou City
  http://www.jiyichem.com/                  Tel: +86-516-89207566                  Fax: +86-516-89207166

_2147483647

