[image: image1.jpg]-

2

BaEE

TONGCHEM





TECHNICAL DATA SHEET           Lemon Chrome Yellow  
Type Yellow Pigment
Delivery Form Powder
Chemical Class Lemon Yellow Pigment  2PbCrO4·PbSO4
Color Index Pigment yellow 34（77603）
CAS No．1344-37-2
Use Recommendation Coating/ Plastics/ Paper/ Print ect.
TECHNICAL DATA
Item                                     Standard 
Water-Soluble Content [%] max                1.0 
Sieve Residue（0.045mm）[%]  max          0.5 
PH Value                                    4.0-8.0
PbCrO4 [%]                    min           50.0
Moisture (After Production) [%]   max           3.0
Oil Absorption [g/100g]          max           25
STANDARD PACKAGING 25kg/bag
TRANSPORT AND STORAGE
Protect against weathering. Store in a dry place and avoid extreme fluctuations in
temperature. Special conditions for opened packaging: Close bags after use to prevent
the absorption of moisture and contamination.
SAFETY
The product is not classified as dangerous under the relevant EC directives and
corresponding national regulations valid in the individual EU member states. It is not
dangerous according to transport regulations. In countries outside the EU, compliance
with the respective national legislation concerning the classification, packaging,
REMARK
This information is given in good faith, without warranty. It is also applies where proprietary rights of third parties are involved. Our advice does not release you from the obligation to verify the information currently provided and to test our products as to their suitability for the intended processes and uses. The application, use and processing of our products and the products manufactured by you on the basis of our technical advice are beyond our control and, therefore, entirely your own responsibility. Our products are sold in accordance with the current version of our General conditions of sale and delivery.
