
[image: image1.png]PRINCEMINERALS




TECHNICAL DATA
  BrickMax CR
Issue dated 4 August 2011
Product:
A high purity manganese oxide powder for colouring of brick and tile and for use in refractory applications.
Appearance:
Extremely fine, brown powder
Particle size (typical):
5 % + 45 µm 
Average particle size:
2 Microns
Absolute density:
4300 kg/m3
Tamped density:
1700 kg/m3 (Typical)
Moisture:
1.0 % (Typical)
                      Typical Chemical Analysis   
Mn……………………................……………….. 69.0 %
Mn3O4……………………………................….... 96.1 %
Fe2O3……...............…………………….……….... 3.5 %
MgO………………...............………………..…… 0.3 %
CaO…………………………...............….……… 0.02 %  
Al2O3………………………..............……..…….. 0.07 %
SiO2…...................................................................... 0.2 %
Typical values are provided in good faith as a guide and should not be taken as a specification. 
The Company reserves the right to change the specification at any time.
Registered in England and Wales No.05582239
Registered office Duke Street Fenton Stoke-on-Trent Staffordshire ST4 3BL

_2147483647

