
[image: image2.png]



RHINOL - 333 
(Silicone Surface Additive) Effects 
	Flow Promotion 
	Better 

	Slip effect 
	Best 

	Anti - crater effect 
	Best 

	Defoaming effect 
	Good 


	Suitability 
: 
	For the manufacture of solvent borne, 2 pack 100%, clear coat & pigmented systems formulations. Less suitable for waterborne & radiation - curing. 

	Lacquer Coat : 
	Suitable for Top Coat. 
Less suitable for Primer or Basecoat. 

	Solubility 
: 
	Clear soluble in Butyl Acetate, Ethanol, TPGDA, Insoluble in White spirit & Water. 


Recommended Addition level 
As supplied calculated on total formulation: 0.1 - 1.0 % 
Processing Instructions 
· Addition to the coating as supplied or as a pre-dilution is possible. 
· Pre-dilution in a suitable solvent simplifies dosage and incorporation. 
Chemical Description 
Polyether siloxane copolymer 
Technical information 

Appearance 
: 
Clear liquid 

Active matter content 
: 
Min 45 % 

Viscosity at 25 0C 
: 
approx. 200 mPas 

Storage stability 
 
  
    When stored in an original unopened packing between -40 and +40 C, 
The product has a shelf life of at least 60 months from the date of manufacture. 
Plot No 





-





 





110





, Chickloli M.I.D.C,





 





Next to Mahanagar  Gas, 





 





Forest Naka, Ambernath 





-





 





W, 





 





Dist 





-





 





Thane (421 505)





 





State 





-





 





Maharashtra, INDIA





 





Ph





 





: +91





-





251





-





268 88





 





11





 





/ 22 / 33





 





Email





 





:





 





rhinol@radiantchemicals.com





 





 





Web





 





:





 www.radiantchemicals.com





 








[image: image1]